## 530 RIPRAP and articulating concrete block revetment systems.

 (REV 5-29-15) (FA 6-8-15) (7-15)

SUBARTICLE 530-1.2 is deleted and the following substituted:

 **530-1.2 Articulating Concrete Block (ACB) Revetment Systems:** Furnish and install an ACB revetment system in accordance with this Section and in conformance with the lines, grades, design, and dimensions shown in the Plans. Submit vendor drawings for review and approval by the Engineer. Provide signed and sealed calculations of the block and cable sizing design for approval. Comply with the National Concrete Masonry Association’s Design Manual for Articulating Concrete Block Revetment Systems, Second Edition, or the National Highway Institute, Hydraulic Engineering Circular (HEC) No. 23, Publication No. FHWA NHI 09-110. Use a minimum Factor of Safety of 1.5 and a maximum 0.5 inch for the block projection.

 Blocks must be open cell and non-tapered unless otherwise stated in the Plans. Revetment cabling must be bi-directional or, for mono-directional cabling, the block installation must include a permanent mechanism within the block matrix to prevent lateral displacement of the installed blocks. Cabling must be polyester and free to move within the block.

 Use only ACB revetment systems currently listed on the Department’s Approved Product List (APL). Manufacturers seeking evaluation of their product shall submit an application in accordance with Section 6, and include certified test reports from an independent test laboratory certifying the ACB revetment system meets the requirements of this Section.

 If the ACB revetment system is intended for use as bridge abutment protection, include the following drawings with the APL submittal:

 1. At the corner transition between the front and side slopes.

 2. For anchorages, geosynthetic materials, treatment of voids between adjacent blocks, limits on void size between adjacent blocks and other special details required to successfully install the ACB.

 3. For areas adjacent to bridge abutments, detail mat placement around curves, connections, protection of mat ends, and splicing of mat.