## STABILIZING (LOCAL AGENCY USE – FDOT ARCHIVE SPECIFICATION).

(REV 01-00) (1-13)

SECTION 160
STABILIZING

160‑1 Description.

 Stabilize designated portions of the roadbed to provide a firm and unyielding subgrade, having the required bearing value specified in the plans. When specified in the plans, provide additional strengthening of the subbase by additional stabilizing of the upper portion of the previously stabilized subgrade, within the limits specified.

160‑2 Stabilized Subgrade.

 For stabilized subgrade, the Contractor may choose the type of material, Commercial or Local.

When the stabilizing is designated as Type B, the Engineer will determine compliance with the bearing value requirements by the Limerock Bearing Ratio (LBR) Method. If approved by the Engineer and only for materials requiring an LBR value of 40, the Engineer may omit Sections 6.0 and 6.1 of Florida Method of Test for Limerock Bearing Ratio (FM 5‑515) and perform an Unsoaked LBR Test. The Engineer or the Contractor may request to use this method. If the Unsoaked LBR Test results in a failing test, then the Engineer will perform a standard Soaked LBR Test. When the stabilizing is designated as Type C, the Engineer will determine compliance by the Florida Soil Bearing Test.

The Contractor is responsible to make the finished roadbed section meet the bearing value requirements, regardless of the quantity of stabilizing materials necessary to be added. Also, the Department will make full payment for any areas where the existing subgrade materials meet the design bearing value requirements without the addition of stabilizing additives, as well as areas where the Contractor may elect to place select high-bearing materials from other sources within the limits of the stabilizing.

After substantially completing the roadbed grading operations, determine the type and quantity (if any) of stabilizing material necessary for compliance with the bearing value requirements. Notify the Engineer of the approximate quantity to be added. Obtain the Engineer's approval for spreading and mixing-in of such quantity of materials to achieve uniformity and effectiveness.

The Engineer may allow, at no additional cost to the Department, the substitution of 6 inches [150 mm] of Granular Subbase meeting the requirements of Section 290, when 12 inches [300 mm] of Type B Stabilization requiring an LBR value of 40 is specified.

160‑3 Stabilized Subbase.

 When Stabilized Subbase is required, after the mixing operations for the stabilization of the entire subgrade limits, strengthen the upper portion of the subgrade, within the limits shown, by adding and mixing-in a loose depth of commercial stabilizing material as designated in the plans or as may be otherwise designated by the Engineer. Provide a minimum depth of spread 3 inches [75 mm] (loose measurement).

160‑4 Materials.

 160‑4.1 Commercial and Local Materials: Meet the requirements of Section 914 for the particular type of stabilizing material to be used.

160‑4.2 Use of Materials from Existing Base: When the use of materials from an existing base is required as all, or a portion, of the stabilizing additives, the Engineer will direct the location, placement, and distribution of such materials. Perform this work prior to the spreading of any additional commercial or local materials. Do not remove any section of existing base until the need for it in maintaining traffic is fulfilled.

The Engineer may direct the Contractor to use materials from an existing base in combination with either of the designated types of stabilizing.

160‑5 Construction Methods.

 160‑5.1 General: Prior to the beginning of stabilizing operations, construct the area to be stabilized to an elevation such that, upon completion of stabilizing operations, the completed stabilized subgrade will conform to the lines, grades, and cross-section shown in the plans. Prior to spreading any additive stabilizing material, bring the surface of the roadbed to a plane approximately parallel to the plane of the proposed finished surface.

The Contractor may process the subgrade to be stabilized in one course, unless the equipment and methods being used do not provide the required uniformity, particle size limitation, compaction, and other desired results, in which case, the Engineer will direct that the processing be done in more than one course.

160‑5.2 Application of Stabilizing Material: When additive stabilizing materials are required, spread the designated quantity uniformly over the area to be stabilized.

When materials from an existing base are to be used in the stabilizing at a particular location, place and spread all of such materials prior to the addition of other stabilizing additives.

Spread commercial stabilizing material by the use of mechanical material spreaders, except that where use of such equipment is not practicable, use other means of spreading, but only upon written approval of the proposed alternate method.

160‑5.3 Mixing: Perform mixing using rotary tillers or other equipment meeting the approval of the Engineer. The Contractor may mix the materials in a plant of an approved type suitable for this work. Thoroughly mix the area to be stabilized throughout the entire depth and width of the stabilizing limits.

Perform the mixing operations, as specified, (either in place or in a plant) regardless of whether the existing soil, or any select soils placed within the limits of the stabilized sections, have the required bearing value without the addition of stabilizing materials.

As an exception to the above mixing requirements, where the subgrade is of rock, the Engineer may waive the mixing operations (and the work of stabilizing), and the Department will not pay for stabilization for such sections of the roadway.

160‑5.4 Maximum Particle Size of Mixed Materials: At the completion of the mixing, ensure that the gradation of the material within the limits of the area being stabilized is such that 97% will pass a 3 inch [90 mm] sieve and that the material does not have a plasticity index greater than eight or liquid limit greater than 30. Note that clay balls or lumps of clay size particles (2 microns or less) [(2 μm or less)] and therefore cannot be considered as individual particle sizes. Remove any materials not meeting the plasticity requirements from the stabilized area. The Contractor may break down or remove from the stabilized area materials not meeting the gradation requirements.

160‑5.5 Compaction: Except where a stabilized subbase is also to be constructed (as specified in 160‑6), after completing the mixing operations and satisfying the requirements for bearing value, uniformity, and particle size, compact the stabilized area in accordance with 160‑8. Compact the materials at a moisture content permitting the specified compaction. If the moisture content of the material is improper for attaining the specified density, either add water or allow the material to dry until reaching the proper moisture content for the specified compaction.

160‑5.6 Finish Grading: Shape the completed stabilized subgrade to conform with the finished lines, grades, and cross-section indicated in the plans. Check the subgrade using elevation stakes or other means approved by the Engineer.

160‑5.7 Requirements for Condition of Completed Subgrade: After completing the stabilizing and compacting operations, ensure that the subgrade is firm and substantially unyielding to the extent that it will support construction equipment and will have the bearing value required by the plans.

Remove all soft and yielding material, and any other portions of the subgrade which will not compact readily, and replace it with suitable material so that the whole subgrade is brought to line and grade, with proper allowance for subsequent compaction.

160‑5.8 Maintenance of Completed Subgrade: After completing the subgrade as specified above, maintain it free from ruts, depressions, and any damage resulting from the hauling or handling of materials, equipment, tools, etc. The Contractor is responsible for maintaining the required density until the subsequent base or pavement is in place including any repairs, replacement, etc., of curb and gutter, sidewalk, etc., which might become necessary in order to recompact the subgrade in the event of underwash or other damage occurring to the previously compacted subgrade. Perform any such recompaction at no expense to the Department. Construct and maintain ditches and drains along the completed subgrade section.

160‑6 Stabilized Subbase (Additional Strengthening of Upper Portion).

 When a stabilized subbase is to be constructed in conjunction with the stabilization operations, after the mixing of the stabilization area as specified in 160‑5.3, and determination that the bearing value requirements specified in 160‑7 have been met, shape the area over which the stabilized subbase is to be constructed as provided in 160‑5.1, and compact it sufficiently to provide a firm surface for the operations to follow. Spread the amount of commercial stabilizing material specified in 160‑3 for this operation, in accordance with 160‑5.2, and mix it to the depth indicated in the plans, in accordance with 160‑5.3. Allow a tolerance of 1 inch [25 mm] in excess of the plan depth in this mixing. The Engineer will not perform any additional tests for bearing value after the mixing of materials for the Stabilized Subbase.

Compact and finish grading, as specified in 160‑5.5 and 160‑5.6, and meet the provisions of 160‑5.4, 160‑5.7, and 160‑5.8 for this work.

When commercial materials are used as the stabilizing additives for the initial subgrade stabilization, the Engineer may eliminate the work of Stabilized Subbase, either entirely or in designated sections of the overall limits for this work as may be specified in the plans.

160‑7 Bearing Value Requirements.

 160‑7.1 General: The Engineer will obtain and test bearing value samples at completion of satisfactory mixing of the stabilized area. For any area where the bearing value obtained is deficient from the value indicated in the plans, in excess of the tolerances established herein, spread and mix additional stabilizing material in accordance with 160‑5.3. Perform this reprocessing for the full width of the roadway being stabilized and longitudinally for a distance of 50 feet [15 m] beyond the limits of the area in which the bearing value is deficient.

The Contractor shall make his own determination of the quantity of additional stabilizing material to be used in reprocessing.

160‑7.2 Tolerances in Bearing Value Requirements: Use the following undertolerances from the specified bearing value, as based on tests performed on samples obtained after completing mixing operations:

|  |  |
| --- | --- |
| Specified Bearing Value | Undertolerance |
| LBR 40 | 5.0 |
| LBR 35 | 4.0 |
| LBR 30 (and under) | 2.5 |
| All Florida Bearing Values | 5.0 |

The following unsoaked bearing value requirement is based on tests performed on samples obtained after completing mixing operations:

|  |  |  |
| --- | --- | --- |
| Specified Bearing Value | Unsoaked Bearing Value Required | Undertolerance |
| LBR 40 | LBR 43 | 0.0 |

160‑8 Density Requirements.

 160‑8.1 General: Within the entire limits of the width and depth of the areas to be stabilized, other than as provided in 160‑8.2, obtain a minimum density at any location of 98% of the maximum density as determined by AASHTO T 180. When bearing value determinations are made by the Florida Soil Bearing Test, the Engineer will use Test Method C of AASHTO T 180, and, when bearing value determinations are made by the Limerock Bearing Ratio Method, the Engineer will use Test Method D of AASHTO T 180 (as modified by the Department's Research Bulletin 22‑B, Revised April, 1972).

160‑8.2 Exceptions to Density Requirements: The Contractor need not obtain the minimum density specified in 160‑8.1 if within the following limits:

(a) The width and depth of areas which are to be subsequently incorporated into a base course under the same contract.

(b) The upper 6 inches [150 mm] of areas to be grassed under the same contract.

Compact these areas to a reasonably firm condition as directed by the Engineer.

160‑9 Method of Measurement.

 160‑9.1 Type B Stabilization and Type C Stabilization: The quantity to be paid for will be the plan quantity, in square yards [square meters], completed and accepted.

160‑9.2 Stabilized Subbase: The quantity to be paid for will be the area, in square yards [square meters], completed and accepted.

160‑9.3 Commercial Stabilizing Material: The quantity to be paid for separately will be determined by measurement, loose volumes, in truck bodies, at the point of unloading.

160‑10 Basis of Payment.

 160‑10.1 Type B Stabilization and Type C Stabilization: Price and payment will constitute full compensation for all work specified in this Section applicable to these types of Stabilization, including furnishing and spreading of all stabilizing material required and any reprocessing of stabilization areas necessary to attain the specified bearing value.

160‑10.2 Stabilized Subbase: Price and payment will constitute full compensation for the work of incorporating the additional commercial stabilizing material into the designated subbase area.

160‑10.3 Commercial Stabilizing Material: Price and payment will be full compensation for furnishing and spreading commercial stabilizing material.

No separate payment will be made for any commercial stabilizing material which the Contractor may elect to use in Type B or Type C Stabilization.

No separate payment will be made for the work of using materials from an existing base, in the stabilizing section.

160‑10.4 General: The above prices and payments will constitute full compensation for all work and materials specified in this Section, specifically including all costs of the processing and incorporation of existing base materials into the proposed stabilization area when such work is required by the plans.

If the item of Borrow Excavation is included in the Contract, any stabilizing materials obtained from designated borrow areas will be included in the pay quantity for Borrow Excavation.

160‑10.5 Payment Items: Payment will be made under:

Item No. 160- 3- Commercial Stabilizing Material - per cubic yard.

Item No. 2160‑ 3‑ Commercial Stabilizing Material ‑ per cubic meter.

Item No. 160- 4- Type B Stabilization - per square yard.

Item No. 2160‑ 4‑ Type B Stabilization ‑ per square meter.

Item No. 160- 5- Type C Stabilization - per square yard.

Item No. 2160‑ 5‑ Type C Stabilization ‑ per square meter.

Item No. 160- 6- Stabilized Subbase - per square yard.

Item No. 2160‑ 6‑ Stabilized Subbase ‑ per square meter.